# Product Information

Copper Phosphorus Silver CP4 Brazing Rods
Brand: Super 6

Product Description

Super 6 CP4 Brazing Rods are premium copper-phosphorus brazing rods enhanced with silver for superior flow, strength, and wetting properties. Designed for capillary brazing of copper and copper alloys, CP4 rods deliver improved joint ductility, electrical conductivity, and mechanical performance. The addition of silver lowers the melting temperature and enhances flow, making CP4 ideal for precise, high-integrity joints in refrigeration, HVAC, and electrical systems.

Key Features

- Copper-phosphorus-silver alloy offering enhanced strength, ductility, and conductivity

- Excellent flow and wetting for smooth, leak-proof capillary brazed joints

- Lower melting range reduces heat input and minimizes distortion

- Self-fluxing on copper – no flux required for copper-to-copper joints

- Supplied in convenient 1kg tube packs for professional use

Typical Applications

- Refrigeration and air conditioning systems

- Electrical and electronic component brazing

- Plumbing and heating installations

- Copper-to-copper and copper-to-brass assemblies

- Precision pipework and high-performance joints

Chemical Composition (% by weight)

| Element | Typical Content |
| --- | --- |
| Copper (Cu) | Approx. 93 – 95% |
| Phosphorus (P) | Approx. 0.8 – 1.3% |
| Silver (Ag) | Approx. 4 – 5% |
| Other | ≤ 0.5% |

## Physical and Technical Data

| Property | Value |
| --- | --- |
| Melting Range | Approx. 620 – 730°C |
| Recommended Brazing Temperature | 600 – 700°C |
| Flux Type | Bare rod (self-fluxing on copper) |
| Suitable Brazing Methods | Oxy-acetylene, torch |
| Joint Strength | High strength, ductile joints |

## Safety and Handling

- Use in well-ventilated areas to avoid inhaling fumes

- Always wear appropriate PPE, including gloves and safety goggles

- Follow all applicable health and safety regulations during use

Liability Notice: Whilst all reasonable efforts have been made to ensure the accuracy of the information contained, this information is subject to change without notice and can be only considered as suitable for general guidance.