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Product Information
Copper Phosphorus Silver CP4 Brazing Rods
Brand: Super 6
Product Description
Super 6 CP4 Brazing Rods are premium copper-phosphorus brazing rods enhanced with silver for superior flow, strength, and wetting properties. Designed for capillary brazing of copper and copper alloys, CP4 rods deliver improved joint ductility, electrical conductivity, and mechanical performance. The addition of silver lowers the melting temperature and enhances flow, making CP4 ideal for precise, high-integrity joints in refrigeration, HVAC, and electrical systems.
Key Features
· Copper-phosphorus-silver alloy offering enhanced strength, ductility, and conductivity
· Excellent flow and wetting for smooth, leak-proof capillary brazed joints
· Lower melting range reduces heat input and minimizes distortion
· Self-fluxing on copper – no flux required for copper-to-copper joints
· Supplied in convenient 1kg tube packs for professional use
Typical Applications
· Refrigeration and air conditioning systems
· Electrical and electronic component brazing
· Plumbing and heating installations
· Copper-to-copper and copper-to-brass assemblies
· Precision pipework and high-performance joints
Chemical Composition (% by weight)
	Element
	Typical Content

	Copper (Cu)
	Approx. 93 – 95%

	Phosphorus (P)
	Approx. 0.8 – 1.3%

	Silver (Ag)
	Approx. 4 – 5%

	Other
	≤ 0.5%






Physical and Technical Data
	Property
	Value

	Melting Range
	Approx. 620 – 730°C

	Recommended Brazing Temperature
	600 – 700°C

	Flux Type
	Bare rod (self-fluxing on copper)

	Suitable Brazing Methods
	Oxy-acetylene, torch

	Joint Strength
	High strength, ductile joints


Safety and Handling
· Use in well-ventilated areas to avoid inhaling fumes
· Always wear appropriate PPE, including gloves and safety goggles
· Follow all applicable health and safety regulations during use













Liability Notice: Whilst all reasonable efforts have been made to ensure the accuracy of the information contained, this information is subject to change without notice and can be only considered as suitable for general guidance.
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