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Product Information
Bronze C5 Brazing Rods
Brand: Super 6
Product Description
The Super 6 Bronze C5 Brazing Rods are high-performance bare rods designed for gas welding and brazing of ferrous and non-ferrous metals where high strength and wear resistance are essential. This copper-tin (phosphor bronze) alloy offers excellent mechanical properties and is ideal for fabricating or repairing components subjected to stress, vibration, and friction in industrial and maintenance applications.
Key Features
· High strength bronze alloy offering excellent wear resistance and toughness
· Bare rod design for use with appropriate flux for controlled, high-quality brazing
· Excellent metallurgical bonding, ideal for steel, cast iron, and copper-based alloys
· Smooth, controlled flow for precise, clean joints with minimal spatter
· Supplied in convenient 5kg packs suitable for workshop and industrial use
Typical Applications
· Heavy-duty fabrication and maintenance
· Agricultural and construction equipment repair
· Steel and copper alloy brazing
· Worn part build-up and surface restoration
· General-purpose gas welding and brazing of dissimilar metals
Chemical Composition (% by weight)
	Element
	Typical Content

	Copper (Cu)
	Approx. 91 – 93%

	Tin (Sn)
	Approx. 5 – 7%

	Phosphorus (P)
	Approx. 0.5 – 1.0%

	Zinc (Zn)
	≤ 1.0%

	Other
	≤ 0.5%




Physical and Technical Data
	Property
	Value

	Melting Range
	Approx. 870 – 940°C

	Recommended Brazing Temperature
	730 – 870°C

	Flux Type
	Use appropriate flux

	Suitable Brazing Methods
	Oxy-acetylene, torch

	Joint Strength
	High mechanical strength


Safety and Handling
· Use in well-ventilated areas to avoid inhaling fumes
· Always wear appropriate PPE, including gloves and safety goggles
· Follow all applicable health and safety regulations during use












Liability Notice: Whilst all reasonable efforts have been made to ensure the accuracy of the information contained, this information is subject to change without notice and can be only considered as suitable for general guidance.
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